| Grip-Engineering info@grip.de | DIN Fixtures Back |
| --- | --- |
| DIN3-8 DIN EN3-8 | Portable fire extinguishers - Part 8: Requirements for the construction, pressure resistance and mechanical tests for extinguishers with a maximum allowable pressure equal to or lower than 30 bar, which comply with the requirements of EN 3-7 | THS1188 |
| DIN34-1 DIN ISO34-1 | Rubber, vulcanized or thermoplastic — Determination of tear strength — Part 1: Trouser, angle and crescent test pieces | THS265-CW THS265-CHV12.7x102 Fig.2 THS1678 |
| DIN178 DIN EN ISO178 | Plastics — Determination of flexural properties | TH103-B220-CR5-oFR5 TH103-B220-CR2-oFR5 TH103-B220-AR2-5-oFR5 TH22 TH238 |
| DIN267 | Fasteners – Technical specification. Tensile strength testing. | THS144 |
| DIN302-3 DIN EN302-3 | Adhesives for load-bearing timber structures - Test methods - Part 3: Determination of the effect of acid damage to wood fibres by temperature and humidity cycling on the transverse tensile strength | THS474-29-76-60-R12.5 |
| DIN306 DIN EN ISO306 | Plastics - Thermoplastic materials - Determination of Vicat softening temperature (VST) | THS265 |
| DIN310 DIN EN310 | Wood-based panels; determination of modulus of elasticity in bending and of bending strength | TH22-5P-CWR2+5x110-CX15-OX30 THS930-20 TH22-500-CX15-oX30 TH22-800-XO15x350-CXU15x350 |
| DIN311 DIN EN311 | Wood-based panels - Surface soundness - Test method | THS325-1 |
| DIN314-1 DIN EN314-1 | Plywood – bonding quality: part 1: test methods | THS1112-EN314-1 |
| DIN319 DIN EN319 | Particleboards and fibreboards; determination of tensile strength perpendicular to the plane of the board | TH16 |
| DIN320 DIN EN320 | Particleboards and fibreboards - Determination of resistance to axial withdrawal of screws | THS325-1 THS325-2 |
| DIN388 DIN EN388 | Protective gloves against mechanical risks | THS174-D20-F1V30-W130 |
| DIN392 DIN EN392 | Glued laminated timber - Shear test glue lines | TH17 |
| DIN408 DIN EN408 | Timber structures - Structural timber and glued laminated timber - Determination of some physical and mechanical properties | THS139-4P-2000-CX30x100-H200 TH22-4P-800-CWX30x300-Af318 |
| DIN433 DIN EN433 | Resilient floor coverings - Determination of residual indentation after static loading | TH23-11,28 |
| DIN455 DIN EN455 | Medical Gloves for Single-Use | TH227 |
| DIN488 DIN EN488 | District heating pipes. Preinsulated bonded pipe systems for directly buried hot water networks. | THS260-150-500-D50-ORxx-Af6030 |
| DIN488-2 | Reinforcing steels - Reinforcing steel bars | THS290-1-3-16 |
| DIN488-5 | Reinforcing steels - Lattice girders. Shear test. Part 2. | THS290-1-3-16 |
| DIN520 DIN EN520 | Gypsum plasterboards - Definitions, requirements and test methods. | TH22-500-CWER5x300-oWER5x300 |
| DIN527-2 DIN EN ISO527-2 | Plastics -- Determination of tensile properties -- Part 2: Test conditions for moulding and extrusion plastics | THS265-CW10x60 THS265-CHB10x60 (Type 1B) THS265-CHB10x80 (Type 1A) THS265-CHB4x25 (Type 5A) THS265-CHB5x30 (Type 1BA) THS474-10-H10-R25 THS1390-ISO527-2-Type1A |
| DIN527-3 DIN EN ISO527-3 | Plastics — Determination of tensile properties — Part 3: Test conditions for films and sheets | THS265-CW THS265-CHB10x60 (Type 1B) THS265-CHB6x33 (Type 5) |
| DIN582 DIN EN582 | Thermal spraying; determination of tensile adhesive strength | THS625 |
| DIN604 DIN EN ISO604 | Plastics - Determination of compressive properties | TH23-56 THS1390-ISO604-Type B |
| DIN763 | Tested, non-calibrated, long-link round steel chains | THS573-20 |
| DIN789 DIN EN789 | Timber structures - Test methods - Determination of mechanical properties of wood based panels | THS1451 |
| DIN813 DIN ISO813 | Determination of adhesion to a rigid substrate - 90 degree peel method | TH95-3 TH95-4 |
| DIN826 DIN EN826 | Thermal insulating products for building applications - Determination of compression behaviour | TH36-400-L6x20 |
| DIN844 DIN EN ISO844 | Rigid cellular plastics — Determination of compression properties | TH23-156-St + THS223g-156 |
| DIN843-1-1 DIN EN843-1-1 | Advanced technical ceramics - Mechanical properties of monolithic ceramics at room temperature - Part 1: Determination of flexural strength | TH238-5P-B200-CWN-ith1 |
| DIN863 DIN EN863 | Protective clothing - Mechanical properties - Test method: Puncture resistance | THS174-D20-F1V30-W130 |
| DIN868-5 DIN EN868-5 | Packaging for terminally sterilized medical devices - Part 5: Sealable pouches and reels of porous materials and plastic film construction | THS1217-V41 + TH240k-Ko+BP30 |
| DIN898-1 DIN EN ISO898-1 | Mechanical properties of fasteners made of carbon steel and alloy steel -- Part 1: Bolts, screws and studs with specified property classes -- Coarse thread and fine pitch thread | THS659-1000 THS786 |
| DIN898-2 DIN EN ISO898-2 | Mechanical properties of fasteners made of carbon steel and alloy steel — Part 2: Nuts with specified property classes — Coarse thread and fine pitch thread | THS786-70 (tensile test) THS659 (tensile test) THS910 (compression test) |
| DIN1170-4 DIN EN1170-4 | Precast concrete products - Test method for glass-fibre reinforced cement - Part 4: Measuring bending strength; "simplified bending test" method | TH103-4P-330-CWEX10-EN1170-4 |
| DIN1193 | Steel hammers - Technical specifications | THS162-910 + TH224+BV |
| DIN1279-4 DIN EN1279-4 | Glass in building - Insulating glass units - Part 4: Methods of test for the physical attributes of edge seal components and inserts | THS504 |
| DIN1288-3 DIN EN1288-3 | Glass in building - Determination of the bending strength of glass - Part 3: Test with specimen supported at two points (four point bending) | THS124-V2-700 |
| DIN1288-5 DIN EN1288-5 | Glass in building - Determination of the bending strength of glass - Part 5: Coaxial double ring test on flat specimens with small test surface areas | THS747-EN1288-5 |
| DIN1293 DIN EN1293 | General requirements for components used in pneumatically pressurized discharge pipes, drains and sewers | THS828-100-4P-30x160 |
| DIN1324 DIN EN1324 | Adhesives for tiles - Determination of shear adhesion strength of dispersion adhesives | THS450 THS534 |
| DIN1348 DIN EN1348 | Adhesives for tiles - Determination of tensile adhesion strength for cementitious adhesives | TH36-50 |
| DIN1372 DIN EN1372 | Test method for adhesives for floor and wall coverings - Peel test | TH192-D20-A26-W57-H38 |
| DIN1464 DIN EN1464 | Adhesives - Determination of peel resistance of adhesive bonds - Floating roller method | TH105-D25-B30 TH105-D30-W45-Af20 |
| DIN1465 DIN EN1465 | Adhesives - Determination of tensile lap-shear strength of bonded assemblies | TH11-5 TH256 |
| DIN1607 DIN EN1607 | Thermal insulating products for building applications - Determination of tensile strength perpendicular to faces | TH113 TH16 |
| DIN1608 DIN EN1608 | Thermal insulating products for building applications - Determination of tensile strength parallel to faces | THS170-500-S200 |
| DIN1719 DIN EN1719 | Adhesives for paper and board, packaging and disposable sanitary products - Tack measurement for pressure sensitive adhesives - Determination of loop tack | THS864-10 |
| DIN1806 DIN EN ISO1806 | Fishing nets - Determination of mesh breaking force of netting | TH231 THS43 |
| DIN1922 DIN EN ISO1922 | Determination of shear properties | TH193-V4 |
| DIN1927-6 DIN EN ISO1927-6 | Monolithic (unshaped) refractory products - Part 6: Measurement of physical properties. 6. Determination of cold crushing strength. | THS223-196 + TH23-196 (for insulating unshaped materials) THS223-96 + TH23-196 (for dense unshaped materials) |
| DIN1939 DIN EN1939 | Self adhesive tapes - Determination of peel adhesion properties | TH50 TH49 THS989-95x45-HR THS1864 |
| DIN2039-1 DIN EN ISO2039-1 | Plastics - Determination of hardness - Part 1: Ball indentation method | THS265 |
| DIN2137 DIN ISO2137 | Rigid cellular plastics — Determination of tensile properties | THS1010-10 |
| DIN-DVS2203-5 | Testing of welded joints ofthermoplastics plates and tubes - Technological bend test | THS260-100-360-D50-OR12.5-Af20 |
| DIN2243-2 DIN EN2243-2 | Petroleum products and lubricants - Determination of cone penetration of lubricating greases and petrolatum | TH105-D25-B30 |
| DIN2243-3 | Aerospace series - Non-metallic materials - Structural adhesives - Test method - Part 3: Peeling test metal-honeycomb core | TH115 |
| DIN2243-4 DIN EN2243-4 | Aerospace series - Non-metallic materials - Structural adhesives - Test method - Part 4: Metal-honeycomb core flatwise tensile test | TH113 |
| DIN2377 DIN EN2377 | Aerospace series; glass fibre reinforced plastics; test method; determination of apparent interlaminar shear strength | THS884+TH238 |
| DIN2439 DIN EN ISO2439 | Flexible cellular polymeric materials — Determination of hardness (indentation technique) | TH36-D200-R1+THS223b-Af159 |
| DIN2493-1 DIN ISO 2493-1 | Paper and board - Determination of bending resistance - Part 1: Constant rate of deflection | THS1445-V3 |
| DIN2562 DIN EN2562 | Aerospace series - Carbon fibre reinforced plastics - Unidirectional laminates; flexural test parallel to the fibre direction | THS884-ith2-Af159 TH238-AR3+OR3+THS884 TH103-B220-CR3-5-oFR3-oFR12.5-ok+GDE |
| DIN2563 DIN EN2563 | Aerospace series - Carbon fibre reinforced plastics - Unidirectional laminates; determination of apparent interlaminar shear strength | TH103-B220-CR3-5-oFR3-oFR12.5-ok+GDE TH238-AR3+OR3+THS884 TH238St-AR3x3-OR3+Gde THS884+TH238+TH187 |
| DIN2759 DIN EN ISO2759 | Board - Determination of bursting strength | THS174-30.5-R5 |
| DIN3037 DIN EN ISO 3037 | Corrugated fibreboard — Determination of edgewise crush resistance (unwaxed edge method) | THS733-200-ISO3037 |
| DIN3303-1 DIN EN ISO3303-1 | Bursting strength of rubber- or plastics-coated fabrics - Part 1: Steel-ball method | THS453-45-P25.2 |
| DIN3327 DIN EN ISO3327 | Hardmetals - Determination of transverse rupture strength | THS1087 TH22St-240-CX5-cgr TH22St-360-CX6-oX6 |
| DIN3377- 2 DIN EN ISO3377- 2 | Leather - Physical and mechanical tests - Determination of tear load - Part 2: Double edge tear | THS694-20 |
| DIN3379 DIN EN ISO3379 | Leather - Determination of distension and strength of surface (Ball burst method) | THS460 |
| DIN3386-1 DIN EN ISO3386-1 | Polymeric materials, cellular flexible - Determination of stress-strain characteristics in compression - Part 1: Low-density materials | THS223k-D203 TH36L-L6x20 |
| DIN3651-2 DIN EN ISO3651-2 | Determination of resistance to intergranular corrosion of stainless steels — Part 2: Ferritic,austenitic and ferritic-austenitic (duplex) stainless steels — Corrosion test in media containing sulfuric acid | TH103-FV-oFR2,3,4,5-W70 |
| DIN3781 DIN ISO3781 | Paper and board -- Determination of tensile strength after immersion in water | THS779-5x60 |
| DIN4108-11 | Thermal insulation and energy economy in buildings - Part 11: Minimum requirements to the durability of bond strength with adhesive tapes and adhesive masses for the establishment of airtight layers | THS1217-V40 (T-peel test) TH49 (180° peel test) |
| DIN4226-1 | Aggregates for concrete and mortar - Part 1: Normal and heavy-weight aggregates | THS994 |
| DIN4226-2 | Aggregates for concrete; aggregates of porous structure (lightweight aggregates); terminology, designation and requirements | THS994 |
| DIN4624 DIN EN ISO4624 | Paints and varnishes, pull off test for adhesion | THS625 THS1514 |
| DIN4843 | Safety footwear; safety requirements, testing | TH124-20 |
| DIN5173 DIN EN ISO5173 | Destructive tests on welds in metallic materials - Bend tests | THS1018 THS260 |
| DIN5299 | Snap hook Karabinerhaken | THS573-20 |
| DIN6259-3 DIN EN ISO6259-3 | Thermoplastics pipes — Determination of tensile properties — Part 3: Polyolefin pipes | THS1086-12-50 THS1086-30-70 |
| DIN6507-2 DIN EN ISO6507-2 | Metallic materials - Vickers hardness test - Part 2: Verification and calibration of testing machines | THS71-10 |
| DIN6872 DIN EN ISO6872 | Dentistry - Ceramic materials | THS1620-16-1.6-ISO6872 |
| DIN6892 DIN EN ISO 6892 | Metallic materials - Tensile testing - Part 1: Method of test at room temperature | THS265-CSS12.7x63 (Type 2) THS265-CSB12.5x75-20x175 (Type 1) |
| DIN6899 | Steel thimbles for fibre ropes Kauschen aus Stahl für Fasereile | THS573-40 |
| DIN7389 DIN EN ISO7389 | Building construction - Jointing products - Determination of elastic recovery of sealants | THS504 |
| DIN7438 DIN EN ISO7438 | Metallic materials — Bend test | TH238-3P-200-CXD30x40 TH103-FV-oRxx-af3816 THS260 THS1711 |
| DIN7808 DIN EN ISO7808 | Plastics - Thermosetting moulding materials - Determination of transfer flow | TH4220-D90+gde |
| DIN 7864 DIN EN ISO7864 | Tensile test fixture to test sterile hypodermic needles | THS1114 THS1180 |
| DIN7886-1 DIN EN ISO7886-1 | Sterile hypodermic syringes for single use - Part 1: Syringes for manual use | THS727-80 TH238-ISO9626 |
| DIN8295 DIN EN ISO8295 | Plastics - Film and sheeting - Determination of the coefficients of friction | TH62-50 |
| DIN8339 DIN EN ISO8339 | Building construction - Sealants - Determination of tensile properties (Extension to break) | THS504 |
| DIN8340 DIN EN ISO8340 | Determination of tensile properties at maintained extension | THS504-52-12-77-36-5 |
| DIN8493 DIN EN ISO8493 | Metallic materials - Tube - Drift-expanding test | THS791 |
| DIN8895 DIN EN ISO 8895 | Shaped insulating refractory products - Determination of cold crushing strength | THS223-196 + TH23-196 |
| DIN9046 DIN EN ISO9046 | Building construction - Jointing products - Determination of adhesion/cohesion properties of sealants at constant temperature | THS504 |
| DIN9073-5 DIN EN ISO9073-5 | Textiles - Test methods for nonwovens - Part 5: Determination of resistance to mechanical penetration (ball burst procedure) | THS453-D44.45-R12.7 |
| DIN9073-7 DIN EN ISO9073-7 | Textiles - Test methods for nonwovens - Part 7: Determination of bending length | THS853-20 |
| DIN9073-18 DIN EN ISO9073-18 | Textiles — Test methods for nonwovens — Part 18: Determination of breaking strength and elongation of nonwoven materials using the grab tensile test | TH83+BG25 |
| DIN9187-1 DIN EN ISO9187-1 | Injection equipment for medical use - Part 1: Ampoules for injectables | TH238-B200-OR2-CWx TH238-ISO9187-1 |
| DIN9626 DIN EN ISO9626 | Stainless steel needle tubing for the manufacture of medical devices - Requirements and test methods | THS1588-ISO9626-Ann.C TH238+CR0.1V90-OR1-St |
| DIN9665 DIN EN ISO 9665 | Adhesives - Animal glues - Methods for sampling and testing | THS42-F12.7R0.39-80 + TH23-56 |
| DIN9836-1 DIN EN ISO9836-1 | Geosynthetics - Determination of thickness at specified pressures - Part 1: Single layers | THS1597 |
| DIN10080 DIN EN10080 | Steel for the reinforcement of concrete - Weldable reinforcing steel - General | THS162-1060-V3-EN10080 |
| DIN10130 DIN EN10130 | Cold rolled low carbon steel flat products for cold forming - Technical delivery conditions | TH192-20-26-W60 |
| DIN10223-3 DIN EN10223-3 | Steel wire and wire products for fencing and netting - Part 3: Hexagonal steel wire mesh products for civil engineering purposes | TH43-G40+W630 |
| DIN10223-8 DIN EN10223-8 | Steel wire and wire products for fencing and netting - Part 8: Welded mesh gabion products | THS290-40 |
| DIN10319 DIN EN ISO10319 | Geosynthetics - Wide-width tensile test | TH135 THS668 |
| DIN10354 DIN EN ISO10354 | Adhesives – Characterization of durability of structural-adhesive-bonded assemblies – Wedge rupture test | THS1455-CH6.5x1-P3x25V60 |
| DIN10477 DIN EN ISO10477 | Dentistry - Polymer-based crown and veneering materials | TH238+CX2+4+10 |
| DIN10545 DIN EN ISO10545 | Ceramic tiles - Part 2: Determination of dimensions and surface quality | TH22-360 |
| DIN11542-2 DIN EN ISO11542-2 | Plastics - Ultra-high-molecular-weight polyethylene (PE-UHMW) moulding and extrusion materials - Part 2: Preparation of test specimens and determination of properties | THS941 |
| DIN11600 DIN EN ISO11600 | Building construction - Jointing products - Classification and requirements for sealants | THS504 |
| DIN11608-3 DIN EN ISO11608-3 | Needle-based injection systems for medical use - Requirements and test methods - Part 3: Finished containers | THS1256-V1 |
| DIN11644 DIN EN ISO11644 | Leather - Test for adhesion of finish | THS1186-20 |
| DIN11979-3 DIN EN ISO11979-3 | Ophthalmic implants - Intraocular lenses - Part 3: Mechanical properties and test methods. Compression test. | THS1486 |
| DIN12002 DIN EN12002 | Adhesives for tiles - Determination of transverse deformation for cementitious adhesives and grouts | TH238-B300-CXH50-D10x60 THS763 |
| DIN12003 DIN EN12003 | Adhesive for tiles - Determination of shear adhesion strength of reaction resin adhesives | THS450 THS534 |
| DIN12004 DIN EN12004 | Adhesives for tiles - Requirements, evaluation of conformity, classification and designation | TH16 THS450 |
| DIN12089 DIN EN12089 | Thermal insulating products for building applications - Determination of bending behaviour | TH22-1300-CX80x300-EN12089-A TH22-600-CX30x150- EN12089-B |
| DIN12090 DIN EN12090 | Shear properties of sandwich core materials | TH193-V4 (Fig. 1) THS608 |
| DIN12190 DIN EN12190 | Determination of compressive strength of repair mortar | TH103-220-CWX10-OWX10 |
| DIN12192 DIN EN ISO12192 | Paper and board — Determination of compressive strength — Ring crush method | THS733-200-ISO12192 |
| DIN12230 DIN EN12230 | Surfaces for sports areas. Determination of tensile properties of synthetic sports surfaces | THS265-CH25x55 |
| DIN12236 DIN EN ISO12236 | Static puncture test on geotextiles | THS174-D150-F50-V2 |
| DIN12242 DIN EN12242 | Touch and close fasteners - Determination of peel strength | THS989-95x45-HR |
| DIN12259-1 DIN EN12259-1 | Fixed firefighting systems - Components for sprinkler and water spray systems - Part 1: Sprinklers | THS1730-V1 |
| DIN12310-1 DIN EN12310-1 | Flexible sheets for waterproofing - Part 1: Bitumen sheets for roof waterproofing; determination of resistance to tearing (nail shank). | THS716 |
| DIN12311-2 DIN EN12311-2 | Flexible sheets for waterproofing - Determination of tensile properties - Part 2: Plastic and rubber sheets for roof waterproofing | THS265-CHB6x33(Type B) |
| DIN12372 DIN EN12372 | Natural stone test methods - Determination of flexural strength under concentrated load | TH103-300-CWX10 |
| DIN12402-Fig1 DIN EN ISO12402-Fig1 | Standard for personal flotation devices | THS1205-9x1.6-Af20 |
| DIN12430 DIN EN12430 | Thermal insulating products for building applications - Determination of behaviour under point load | TH23-79.8 TH36-300-QZ100-Al + THS223k-79.8R0.5-Af159 |
| DIN12431 DIN EN12431 | Thermal insulating products for building applications. Determination of thickness for floating floor insulating products | TH36-200 |
| DIN12467 DIN EN12467 | Fibre-cement flat sheets - Product specification and test methods | TH22-360+FD30x250 TH22St-5P-800-CWX10+CWX40x500+CWLD30x120 |
| DIN12625-5 DIN EN ISO12625-5 | Tissue paper and tissue products - Part 5: Determination of wet tensile strength | THS779-5x60 |
| DIN12625-9 DIN EN ISO12625-9 | Tissue paper and tissue products - Part 9: Determination of ball burst strength | THS855-10 |
| DIN12773 DIN EN12773 | Footwear - Test methods for outsoles - Needle tear strength | THS111 |
| DIN12814-2 DIN EN12814-2 | Testing of welded joints of thermoplastics semi-finished products - Part 2: Tensile test | THS260-100-360 |
| DIN12814-4 DIN EN12814-4 | Testing of welded joints of thermoplastics semi-finished products - Part 4: Peel test | THS353-5x30 (Fig.5 ) |
| DIN13055-1 DIN EN13055-1 | Lightweight aggregates - Part 1: Lightweight aggregates for concrete, mortar and grout | THS994 |
| DIN13354 DIN EN13354 | Solid wood panels (SWP) - Bonding quality | THS740 |
| DIN13393 DIN EN13393 | Packaging - Specification for edge protectors | THS993-240 |
| DIN13446 DIN EN13446 | Wood-based panels - Determination of withdrawal capacity of fasteners | THS325+THS235-20-130x130 |
| DIN13503-2 DIN EN ISO13503-2 | Petroleum and natural gas industries -- Completion fluids and materials - Part 2: Measurement of properties of proppants used in hydraulic fracturing and gravel-packing operations | THS947 |
| DIN13523-1 DIN EN13523-1 | Coil coated metals - Test methods - Part 1: Film thickness | TH4060 |
| DIN13555 DIN EN13555 | Flanges and their joints - Gasket parameters and test procedures relevant to the design rules for gasketed circular flange connections | THS1510 |
| DIN13572 DIN EN13572 | Footwear - Test methods for uppers, lining and insocks - Seam strength | THS1205 |
| DIN13892-2 DIN EN13892-2 | Methods of test for screed materials - Part 2: Determination of flexural and compressive strength | TH103-200-CWEX10-OWEX10 |
| DIN13934 DIN EN ISO13934 | Textiles - Tensile properties of fabrics - Part 1: Determination of maximum force and elongation at maximum force using the strip method | TH83 THS265-CHR50x260 |
| DIN13936-1 DIN EN ISO13936-1 | Textiles - Determination of the slippage resistance of yarns at a seam in woven fabrics - Part 1: Fixed seam opening method | TH240g+B25x25+B25x50 |
| DIN13936-2 DIN EN ISO13936-2 | Textiles - Determination of the slippage resistance of yarns at a seam in woven fabrics - Part 2: Fixed load method | TH240g+BP25x25+BP25x50 TH240k+BW30+BW50 |
| DIN13936-3 DIN EN ISO13936-3 | Textiles - Determination of the slippage resistance of yarns at a seam in woven fabrics - Part 3: Needle clamp method | THS1108 |
| DIN14024 DIN EN14024 | Metal profiles with thermal barrier. Mechanical performance. Requirements, proof and tests for assessment | THS1273 (Tensile test) THS674-V4 (Shear test) |
| EN14080 DIN EN14080 | Timber structures - Glued laminated timber and glued solid timber - Requirements Timber structures - Glued laminated timber and glued solid timber - Requirements | TH17 |
| DIN14125 DIN EN ISO14125 | Fibre-reinforced plastic composites - Determination of flexural properties | TH22-5P-240-CWLD4+D10 TH22-5P-CWR2+110 Fig 4 THS884+TH238+TH187 |
| DIN14126 DIN EN ISO14126 | Fibre-reinforced plastic composites - Determination of compressive properties in the in-plane direction | THS705+Ko THS613 (Method 1) THS793-ISO14126 (Method 2 Fig. C2) THS321-250c-Hy + THS705-F100-Ko TH121 |
| DIN14130 DIN EN ISO14130 | Fibre reinforced plastic composites - Determination of apparent interlaminar shear strength by short beam-method | TH103-B220+AR2R5 THS884-ith2-Af159 |
| DIN14272 DIN EN ISO14272 | Resistance welding - Destructive testing of welds - Specimen dimensions and procedure for cross tension testing of resistance spot and embossed projection welds | THS1146 |
| DIN14279 DIN EN14279 | Laminated Veneer Lumber (LVL) - Definitions, classification and specifications | THS927 |
| DIN14410 DIN EN14410 | Self adhesive tapes - Measurement of breaking strength and elongation at break | THS919-100 THS919-100-100-F20 |
| DIN14444 DIN EN14444 | Structural adhesives - Qualitative assessment of durability of bonded assemblies - Wedge rupture test | THS1455-CH6.5x1-P3x25V60 |
| DIN14704-1 DIN EN14704-1 | Determination of the elasticity of fabrics - Part 1: Strip tests | TH231-D6+R8-W80 (Loop test) THS353-6x80-Al (Loop test) TH240g+BLCR3-25x75 (Strip test) TH227-B80-BLCR3 (Strip test) |
| DIN14477 DIN EN14477 | Packaging, Flexible packaging material - Determination of puncture resistance - Test methods | THS511 |
| DIN14509 DIN EN14509 | Self-supporting double skin metal faced insulating panels - Factory made products - Specifications | TH22-1300-500-CN40x200 TH22-1000-360-CM60x160-H200 THS1063-20.3-WDF |
| DIN14555 DIN EN ISO14555 | Welding - Arc stud welding of metallic materials | THS1556 |
| DIN14801 DIN EN ISO14801 | Dentistry - Implants - Dynamic loading test for endosseous dental implants | THS543-170 THS1447-V2-ISO14801 |
| DIN14891 DIN EN14891 | Liquid applied water impermeable products for use beneath ceramic tiling bonded with adhesives. Requirements, test methods, assessment and verification of constancy of performance, classification and marking | THS1168-Am1665 |
| DIN14916 DIN EN ISO14916 | Thermal spraying - Determination of tensile adhesive strength | THS625 THS1514 |
| DIN15048-1 DIN EN15048-1 | Non-preloaded structural bolting assemblies - Part 1: General requirements | THS786 |
| DIN15630-2 DIN EN ISO15630-2 | Steel for the reinforcement and prestressing of concrete - Test methods - Part 2: Welded fabric and lattice girder | THS290-10 THS290-21 THS290-30 THS290-40 THS290-50 |
| DIN CEN/TR 16792-Fig.B5 | Safety of children's clothing - Recommendations for the design and manufacture of children's clothing - Mechanical safety. Button pull-off test | THS807-S25 + THS1042-30 THS1042-10 + TH240k+BP25+BP50 |
| DIN17271 DIN EN17271 | Plastics - Poly(vinyl chloride) (PVC) based profiles - Determination of the peel strength of profiles laminated with foils | TH192-25-27-180-180-4R |
| DIN17333-4 DIN EN17333-4 | Characterization of One Component Foam (OCF) - Part 1: Yield Measurement of the tensile strength of polyurethane foam Charakterisierung von Einkomponentenschäumen Messung der Zugfestigkeit von Polyurethanschaum | THS504-62-82-200-5-Af20-EN17333-4-M2 |
| DIN17697 DIN EN ISO17697 | Footwear - Test methods for uppers, lining and insocks - Seam strength | THS1205 |
| DIN18134 | Soil - Testing procedures and testing equipment - Plate load test | TH4020 |
| DIN18164-1 | Cellular plastics as insulating building materials; insulating materials thermal insulation | THS170 |
| DIN19304 | Testing of corrugated board-Creasings | THS1489-V2 |
| DIN19736 DIN ISO19736 | Dentistry - Bonding test between polymer teeth and denture base materials | THS1959-ISO19736 |
| ISO20126 DIN EN ISO20126 | Dentistry — Manual toothbrushes — General requirements and test methods | THS341-10-K + THS63-10 |
| DIN20482 DIN EN ISO20482 | Testing of metals; Erichsen cupping test on sheet and strip metal having a width of >= 90 mm; Thickness range: 0.2 mm to 2 mm | THS145-D27-R10 THS145-D11-R4 |
| DIN20795-1 EN ISO20795-1 | Dentistry - Artificial teeth for dental prostheses | THS1447-S12 + TH227+BP25-Af20 |
| DIN21182 DIN EN ISO21182 | Light conveyor belts - Determination of the coefficient of friction | TH62-40 |
| DIN22112 DIN EN ISO22112 | Dentistry - Artificial teeth for dental prostheses | THS1447-S12 + TH227+BP25-Af20 |
| DIN22254 DIN EN ISO22254 | Dentistry - Manual toothbrushes - Resistance of tufted portion to deflection | THS63-Z3 |
| DIN23910 DIN EN ISO23910 | Leather - Physical and mechanical tests - Measurement of stitch tear resistance | THS694-10 |
| DIN23936-2-B.2 DIN EN ISO23936-2-B.2 | Petroleum, petrochemical and natural gas industries - Non-metallic materials in contact with media related to oil and gas production - Part 2: Elastomers | THS1512-325 |
| DIN28510-1 DIN EN28510-1 | Adhesives - Peel test for a flexible-bonded-to-rigid test specimen assembly - Part 1: 90° peel | TH50 |
| DIN29022 DIN EN ISO29022 | Dentistry - Adhesion - Notched-edge shear bond strength test | THS633-540-V5 |
| DIN29862 DIN EN ISO29862 | Self adhesive tapes - Determination of peel adhesion properties | THS989-95x45-HR |
| DIN40802-1 | Metal-clad base material for printed circuits;specifications | TH249-12-25 |
| DIN50101-1 | Testing of metals; Erichsen cupping test on sheet and strip metal having a width of >= 90 mm; Thickness range: 0.2 mm to 2 mm | THS145-D27-R10 |
| DIN50101-2 | Testing of metals; Erichsen cupping test on sheet and strip metal having a width of >= 90 mm; Thickness range: over 2 mm up to 3 mm | THS145-D40-R10 |
| DIN50109 | Tensile testing of lamellar graphite cast iron | TH179-63-8 |
| DIN50114 | Testing of metals; tensile test on sheet or strip without using an extensometer | TH135 |
| DIN50125 | Testing of metallic materials - Tensile test pieces | THS800-120 TH89-20 TH89-3816 THS565-60 THS474-12.5x20 THS885-70 THS265-CSB20x60-27-100 |
| DIN50141 | Testing of metals; Shear test | THS396 |
| DIN50146 DIN EN50146 | Cable ties for electrical installations | THS43-H40 |
| DIN50139 | Testing of Steel; Flanging Test on Tubes | THS791-A60xD148-Af6025 + TH23 |
| DIN50342-5 DIN EN50342-5 | Lead-acid starter batteries - Part 5: Properties of battery housings and handles | THS1402 (4.4.4) |
| DIN52186 | Testing of wood- Bending test | TH22-WNJ30 |
| DIN52187 | Testing of wood; determination of ultimate shearing stress parallel to grain | THS740 TH17 |
| DIN52292-1 | Testing of glass and glass ceramics; determination of bending strength; coaxial double ring bending test on flat specimens with small test area | THS747-30-90-R2.5-DIN52292-Am1665 +THS800-200x200x150 |
| DIN52352 | Testing of wood fibre boards; bend testing | TH22-1200-CJ50x120 |
| DIN52365 | Testing of wood chipboards; determination of tensile strength vertical to the chipboard plane | TH16 |
| DIN52367 | Wood-based panels - Determination of shear strength parallel to the surface | TH17 |
| DIN52371 | Testing of plywood; bending test | TH22 |
| DIN52377 | Testing of plywood - Determination of modulus of elasticity in tension and of tensile strength | TH83 |
| DIN52455-3 | Testing of sealants in building construction - Adhesion and extension test - Part 3: Influence of light through glass | THS504 |
| DIN53121 | Testing of paper and board - Determination of the bending stiffness by the beam method | THS1119 |
| DIN53142-2 | Testing of board - Puncture test - Part 2: Puncture test with linear move | THS174-Tr100-Pr60x25 |
| DIN53278 | Testing of adhesives for floor coverings; testing of peel-resistance of bondings, reaction adhesives for rubber floor-coverings described in DIN 16852 | TH249-12-25 |
| DIN53289 | Rollenschälversuch | TH105-D25-B30 |
| DIN53292 | Testing of sandwiches; Tensile test perpendicular to the faces | TH113 |
| DIN53293 | Testing of sandwiches; Bending test | TH22-5P-CWR2+110 Fig 4 |
| DIN53294 | Shear properties of sandwich core materials | TH193-V6 |
| DIN53295 | Peel resistance of adhesive bonds, e.g. for honeycomb sandwich constructions | TH115 |
| DIN53331 | Leather - Measurement of stitch tear resistance | THS694-10 |
| DIN53357 | Testing of plastics sheets; adhesion test | TH3-90 |
| DIN53362 | Testing of plastics films and textile fabrics (excluding nonwovens), coated or not coated fabrics - Determination of stiffness in bending - Method according to Cantilever | THS853-20 |
| DIN53375 | Testing of plastic film and sheeting; determination of the coefficients of friction | TH62-F |
| DIN53430 | Testing of Rigid Cellular Materials; Tensile Test | TH213 |
| DIN53494 | Electroplated coatings; testing of electroplated plastic articles; determination of peel strength | TH104-30 |
| DIN53504 | Testing of rubber - Determination of tensile strength at break, tensile stress at yield, elongation at break and stress values in a tensile test | TH44 THS265-CW THS265-CHB4x25 (S2) THS265-CHB6x33 |
| DIN53506 | Testing of rubber; determination of needle tear resistance | THS111 |
| DIN53515 | Determination of tear strength of rubber elastomers and plastic film using Graves angle test piece with nick | THS265-CW THS265-CHV12.7x102 |
| DIN53531-1 | Determination of the adhesion of rubber to rigid materials by the one-plate method | TH95-3 TH95-4 |
| DIN53579-2 | Testing of flexible cellular materials; hardness test on finished parts; compression test on profiles | THS223b-112.8 |
| DIN53769-1 | Testing of glass fibre reinforced plastics pipes; determination of the longitudinal shear strength of type B pipe fittings | THS1709 |
| DIN53857 | Testing of textiles; simple tensile test on strips of textile fabrics, woven fabrics and ribbons | TH83 |
| DIN53858 | Testing of textiles; determination of the breaking strength of textile fabrics (with the exception of nonwoven textiles), grab method | TH83 |
| DIN54307 (superseded by ISO12236) | Testing of geotextiles and geotextile related products; static puncture test (CBR) (proposal for a European Standard) | THS174-150 |
| DIN54516 | Testing of paper and board - Determination of plybond resistance | THS87-30 |
| DIN60793-1-32 DIN EN/IEC 60793-1-32 | Optical fibres - Part 1-32: Measurement methods and test procedures - Coating strippability | THS1192+Ko + TH76-1-D80+Ko |
| DIN61061-1 DIN EN61061-1 | Non-impregnated densified laminated wood for electrical purposes - Part 1: Definitions, designation and general requirements | THS949 |
| DIN61386-1 DIN EN61386-1 | Conduit systems for cable management - Part 1: General requirements | TH16-99-D64-W100 (Tensile test) TH23-Q50-R1-Af20-ST (Compression test) |
| DIN65561 | Aerospace; fibre reinforced plastics; testing of multidirectional laminates; determination of compressive strength after impact test | THS818 |
| DIN68501 | Hardware for furniture - Test methods for determination of strength and stiffness of cabinet connectors | THS1576 |
| info@grip.de LX 17 Apr 2024 |  | TOP |